GOVERNING CODES AND REGULATIONS

- 管理规范和条例

SANS 10244-2 (BS EN 10244-2): Steel wire and wire products-Non ferrous metallic coatings on steel wire Part 2 Zinc or zinc alloy coatings.

  - SANS 10244-2（BS EN 10244-2）：钢丝和钢丝制品钢丝上的有色金属涂层第2部分锌或锌合金涂层。

SANS 10025-2: Hot rolled products of structural steels

  - SANS 10025-2：结构钢热轧产品

SANS 23-4: Steel wire and wire products for fences Part 4: Steel wire welded mesh fencing.

  - SANS 23-4：围栏用钢丝和钢丝制品第4部分：钢丝焊接网围栏。

SANS 121 (ISO 1461): Hot dip galvanised coating on fabricated iron and steel articles-Specifications and test methods.

  - SANS 121（ISO 1461）：预制钢铁制品的热浸镀锌涂层规范和试验方法。

SANS 1700-5-8: Fasteners Part 5: General requirements and mechanical properties Section 8: Mechanical properties of corrosion resistant stainless steel fasteners-Bolts, screws and studs.

  - SANS 1700-5-8：紧固件第5部分：一般要求和机械性能第8节：耐腐蚀不锈钢紧固件的机械性能螺栓、螺钉和螺柱。

## Corner - Gate - Straining Posts

## 转角-门-拉紧柱

Fabricated from tubular steel pipe, 100mm dia. X 2mm thick, 2.6m in height plus an overhang of 450mm set at 45o.

- 由直径100mm的钢管制成。X 2mm厚，2.6m高，45°处有450mm的悬垂。

Top of pole to have a mushroom cap fitted and the bottom to have a base plate welded to it, posts shall be holed for wires and stay bolts as required.

- 电杆顶部应安装蘑菇盖，底部应焊接底板，立柱应按要求开孔，以便安装电线和拉线螺栓。

Unless otherwise specified, the posts shall be painted with two coats aluminium paint, the base plate and the portion of the pole to be planted in the ground shall be well tarred.

- 除非另有规定，否则柱子应涂上两层铝漆，底板和杆的埋入地面部分应涂上良好的柏油。

Straining posts shall be planted as specified but will not exceed 50 metres spacings.

- 应按规定种植拉紧柱，但间距不得超过50米。

All posts will be embedded in a 400 X 400 X 600mm class B concrete block.

- 所有立柱将嵌入400 X 400 X 600mm的B级混凝土块中。

## Stays

## 保持

Fabricated from tubular steel pipe, 50mm dia. X 2mm thick X 3.050m long.

- 由直径50mm的管状钢管制成。X 2毫米厚X 3.050米长。

The top of the pole will be flattened and a hole drilled for a 10mm stay bolt.

- 将电杆顶部压平，并钻一个10毫米的撑杆螺栓孔。

The bottom of the pole will have a base plate welded on to it.

- 电杆底部将焊接一块底板。

Painting will be the same as 2.3 above for posts.

- 柱子的涂装将与上述2.3相同。

Unless otherwise specified, corner and straining posts shall be fitted with two stays.

- 除非另有规定，否则角柱和拉紧柱应配备两根撑杆。

Gate and end posts with one stay each.

- 门柱和端柱各有一根撑杆。

All posts will be embedded in a 300 X 300 X 300mm class B concrete block.

- 所有立柱将嵌入300 X 300 X 300mm的B级混凝土块中。

## Iscor Standards

## Iscor标准

Approved “Y” type mild steel standards 2.450m long with a 450mm overhang welded on at a 45o angle.

- 经批准的“Y”型低碳钢标准2.450m长，450mm悬垂以45o角焊接。

Standards will be painted with two coats of bitumastic paint.

- 标准件将涂上两层沥青漆。

Standards will be driven into the ground to a depth of 600mm and will be spaced at intervals not exceeding four metres.

- 标准将被打入地下600mm深，间距不超过4m。

## Intermediate Posts (alternative to the Iscor “Y” type standard)

## 中级职位（Iscor“Y”型标准的替代品）

Fabricated from tubular steel pipe, 50mm dia. X 2mm thick, 2.4m in height plus an overhang of 450mm set at 45o.

- 由直径50mm的管状钢管制成。X 2mm厚，2.4m高，45°处有450mm的悬垂。

Top of pole to have a mushroom cap fitted and the bottom to have a base plate welded to it, posts shall be holed for wires and stay bolts as required.

- 电杆顶部应安装蘑菇盖，底部应焊接底板，立柱应按要求开孔，以便安装电线和拉线螺栓。

Unless otherwise specified, the posts shall be painted with two coats aluminium paint, the base plate and the portion of the pole to be planted in the ground shall be well tarred.

- 除非另有规定，否则柱子应涂上两层铝漆，底板和杆的埋入地面部分应涂上良好的柏油。

Intermediate posts shall be planted as specified but will not exceed four metre spacings.

- 中间立柱应按规定种植，但间距不得超过4米。

All posts will be embedded in a 300 X 300 X 450mm class B concrete block.

- 所有立柱将嵌入300 X 300 X 450mm的B级混凝土块中。

Wire Mesh Fencing

- 铁丝网围栏

Wire mesh fencing shall be 1.8m high plus a 450mm overhang.

- 铁丝网围栏应高1.8m，悬垂450mm。

Four strands of tightly strained 4mm wire will be tied to the posts and standards.

- 四股绷紧的4mm钢丝将系在柱子和标准上。

Galvanised diamond mesh wire 64mm X 2.5mm will be used to cover the four strands of tightly strained wire and will be tied in position with 1.6mm tie wire.

- 将使用64mm X 2.5mm的镀锌菱形钢丝网覆盖四股拉紧的钢丝，并用1.6mm的绑线将其绑扎到位。

Galvanised diamond mesh will be in long lengths and no jointing of mesh will be done without the approval of the Project Engineer.

- 镀锌金刚石网将是长的，未经项目工程师批准，不得进行网的连接。

The overhang will consist of three strands of 2.5mm X 2mm barbed wire tightly strained and tied to the post overhangs.

- 悬挑将由三股2.5mm X 2mm的带刺铁丝网组成，这些铁丝网紧紧地拉紧并绑在立柱悬挑上。

Double and Single Gates

- 双扇门和单扇门

Gates will be manufactured from 42.8mm dia X 2mm steel pipe.

- 闸门将由直径42.8mm X 2mm的钢管制成。

The corners will be mitred.

- 角落将被斜接。

Bracing will be made out of 21.4mm dia. steel pipe.

- 支架将由直径21.4mm的材料制成。钢管。

Galvanised diamond mesh will be used to cover the frame and it will be fixed with 1.6mm tie wire.

- 镀锌菱形网将用于覆盖框架，并用1.6mm的绑线固定。

Security overhangs will be fitted to the gate to match the fence.

- 大门将安装安全悬挑，与围栏相匹配。

The gate frames will be painted with two coats of aluminium paint.

- 门框将涂上两层铝漆。

Unless specified, single gates shall be 1.2 metres and double gates 4.270 metres wide.

- 除非另有规定，否则单扇门的宽度应为1.2米，双扇门的宽度为4.270米。

Straining Bolts

- 拉紧螺栓

Straining bolts shall be 300mm X 10mm and galvanised.

- 拉紧螺栓应为300mm X 10mm并镀锌。